## Slide 1: Machine learning techniques for predicting the properties of ceramic products
Pedro Domingues
Petia Georgieva
Institute of Telecommunications/Institute of Electronics and Informatics Engineering of Aveiro/Department of Electronics, Telecommunications and Informatics, University of Aveiro, 3810-193 Aveiro, Portugal

## Slide 2
Introduction and Motivation
Corbário motivated (ask what phrase was)
Laboratory trial and error costly and timely
Reduce number of laboratory trials

## Slide 3
Dataset
230 ceramic formulations
  7 raw materials each with 11 features
  4 target features (Aluminum Oxide(Al2O3), Iron(III) Oxide (Fe2O3), carbon and dry-to-fired shrinkage
Most of the ceramic formulations don’t include all the raw materials leading to a high number of zeros

## Slide 4
Linear Regression
  Simpler Model
  One target predicted at a time.
  Predicted for:
    Features with correlation bigger 0.1
    First 3 raw materials
    Direct features (Using Al2O3 to predict Al2O3, Fe2O3 to predict Fe2O3 and Carbon to predict Carbon)
Neural Network
  More robust model
  All targets predict at the same time
  Predicted for:
    All features
    5 raw materials (excluding most zeros instead of converting them to a small value)
    Most used raw materials
    Direct features and their percentage of usage for the 7 raw materials
    Direct features and their percentage of usage for the 5 raw materials
ML Models: Linear Regression vs Neural Network

## Slide 5
Results for linear regression
Features | Target | MAE | MSE | R2
Corr > 0.1 | Al2O3 | 0.486114 | 0.351496 | 0.496937
3 raw materials | Al2O3 | 0.514595 | 0.405854 | 0.419139
Al2O3 only | Al2O3 | 0.572654 | 0.507638 | 0.273466
3 raw materials | Carbon | 0.030292 | 0.001731 | 0.11239
D-F Shrinkage only | D-F Shrinkage | 0.343777 | 0.182973 | 0.015371
Carbon only | Carbon | 0.032272 | 0.001955 | -0.002301
Corr > 0.1 | Carbon | 0.032283 | 0.001976 | -0.013284
3 raw materials | D-F Shrinkage | 0.346842 | 0.209531 | -0.127547
Fe2O3 only | Fe2O3 | 0.097849 | 0.014264 | -0.248736
3 raw materials | Fe2O3 | 0.102115 | 0.015396 | -0.34779
Corr > 0.1 | Fe2O3 | 0.109827 | 0.019705 | -0.724988
Corr > 0.1 | D-F Shrinkage | 0.518506 | 0.425968 | -3.150945

## Slide 6
Results for neural networks
Features | MSE | MAE | R2
Related features 7 raw materials | 0.285683 | 0.263759 | 0.998125
All features | 0.269828 | 0.305901 | 0.997691
Related features 5 raw materials | 0.679531 | 0.430052 | 0.995540
All Features | 0.815669 | 0.485576 | 0.993019
3 raw materials | 1.710167 | 0.664238 | 0.985364

## Slide 7
Takeaways
  Neural networks proved capable of predicting ceramic properties
  Potential to help streamline production
Future work
  More data preprocessing
  New data to test this models on
Acknowledgements
  Corbário – Industrial Minerals for providing the dataset